FRICK NG 1

PRODUCT DESCRIPTION

Frick NG 1 is a custom-blended, highly refined, chemically resistant lubricant.  State of the art additives act as lubricity improvers, defoamants, and pour point depressants.  It also helps protect the metal surfaces against corrosion.  This product is widely used in environments and certain applications (e.g. flooded rotary screw compressors) where shear stability, lubricity and resistance to chemical attack by the compressed gas are required.

APPLICATIONS
--
Lubricant/coolant for process and hydrocarbon gas rotary screw compressors.  

--
Proprietary additive helps to protect metal surfaces from corrosive attack by sour 


gas (H2S).

TYPICAL PROPERTIES*




Viscosity @ 40°C cs ASTM D445


97

Viscosity @ 100°C cs


11.8

Viscosity @ 100°F


108.6

Viscosity @ 210°F


12.1

Viscosity Index ASTM D2270


111

Density, lb/gal, 60°F


7.42

Pour Point °F (°C) ASTM D97


-10°F (-23°C)

Flash Point, C.O.C., °F (°C) ASTM D92


465 (240)

Fire Point, C.O.C., °F (°C) ASTM D92


510 (265)

Specific Gravity, ASTM D1298


0.890

*These values are not intended for use in preparing specifications.

6/99
