FRICK NG 2

PRODUCT DESCRIPTION

Frick NG 2 product is custom-blended, highly refined, dewaxed, chemically inert lubricants.  Silicone additions act as a lubricity improver, defoamant, pour point depressant and help protect the metal surfaces against corrosion.  Widely used for applications where the lubricant is subjected to harsh chemical environments.  Contains an additive compatible with sour hydrocarbon (H2S) gas systems.

APPLICATIONS
--
Lubricant/coolant for process and gas rotary screw compressors.

--
Lubricant/coolant for process applications.  Especially effective in combating


corrosion and promoting long life in sour hydrocarbon gas compressors.

TYPICAL PROPERTIES*





Viscosity @ 40°C cs ASTM D445

93



Viscosity @ 100°C cs

11.7



Viscosity @ 100°F

104



Viscosity @ 210°F

12.0



Viscosity Index ASTM D2270

116



Density, lb/gal, 60°F

7.4



Pour Point °F (°C) ASTM D97

-35 (-37)



Flash Point, C.O.C., °F (°C) ASTM D92

470 (243)



Fire Point, C.O.C., °F (°C) ASTM D92

515 (268)



Specific Gravity, ASTM D1298

0.89



*These values are not intended for use in preparing specifications.

6/99
